## Slide 1: Sheet Forming Processes

## Slide 2: Basic Categories
Shearing
Bending
Drawing

## Slide 3: Standard Punching Operation

## Slide 4: Conventionally Sheared Surface

## Slide 5: Fineblanking Process

## Slide 6: Fineblanked Part

## Slide 7: Power Shear

## Slide 8: Piercing vs. Blanking

## Slide 9: Piercing, Lancing and Blanking

## Slide 10: Blanking Punch Design

## Slide 11: 5-Station Progressive Piercing, Forming and Cut-off Punch and Die

## Slide 12: Stages of 11-Station Progressive Punch and Die

## Slide 13: Bar Folder

## Slide 14: Press Brake

## Slide 15: Bent Sheet Profiles

## Slide 16: Dies Forming a Rolled Bead

## Slide 17: Roll Bending

## Slide 18: Bend Sheets into Shapes

## Slide 19: Forming a Box Channel

## Slide 20: Sheet Metal Seaming

## Slide 21: Straightening Sheets and Strips

## Slide 22: Forming Sheet by Spinning

## Slide 23: Forming a Reflector by Spinning

## Slide 24: Shear Forming

## Slide 25: Stretch Forming

## Slide 26: Deep Drawing

## Slide 27: Metal Flow in Drawing

## Slide 28: Piercing, Blanking, Drawing and Trimming

## Slide 29: Hydroforming Sheets

## Slide 30: Hydroforming Tubes

## Slide 31: Cross-section of Formed Tube

## Slide 32: Formed Tubes in Auto Bodies

## Slide 33: Hot Drawing

## Slide 34: Ironing

## Slide 35: Embossing